# FASTCHIP SEMICONDUCTOR — TECHNICAL REPORT

Document ID: TR-PE-2026-0088

Title: Volta-7 Yield Improvement Report — Q1 2026

Author: James Ortiz, Lead Yield Engineer, Product Engineering Division

Reviewed By: Lisa Park, PE Manager | Mike Chen, VP Product Engineering

Date: March 29, 2026

Classification: Confidential — Internal Engineering Distribution Only

Target Product: Volta-7 Automotive EV Powertrain Controller (Rev A Silicon)

# 1. Executive Summary & Yield Progression

During the initial silicon introduction phase of the Volta-7 automotive powertrain controller in January 2026, first-silicon probe yield at wafer sort opened at an unacceptable baseline of 41.2% across Lot LOT-V7-001 (25 wafers, 200mm BCD 130nm process node at Penang Fab 2). This baseline fell significantly below the commercial ramp entitlement model of 70.0% packageable die yield required for Tier-1 automotive customer NovaDrive Motors.

Through focused physical failure analysis, spatial wafer inline defect inspection, and cross-functional engineering execution between Austin Product Engineering and Penang Fab Operations, the primary yield loss mechanism was isolated to Chemical-Mechanical Planarization (CMP) over-polishing on the Metal 3 copper layer. Process corrections implemented in Penang Fab Platen-1/Platen-2 polishing regimes reduced inline defectivity by 68%, elevating gross probe yield to 54.8% by mid-February (Lot LOT-V7-004) and reaching 58.2% by late March (Lot LOT-V7-013). This report provides detailed yield trend diagnostics, defect pareto classification, root cause physics, and process control actions implemented to support the Rev B ramp targeting >75% yield.

Volta-7 Q1 2026 Yield Progression Trend

+-------------------------------------------------------------------------+
| Yield (%)                                                               |
|  80 |                                                                   |
|  70 | - - - - - - - - Target Baseline: 70.0% - - - - - - - - - - - - - -|
|  60 |                                                  [58.2%] LOT-V7-13|
|  50 |                                 [54.8%] LOT-V7-04                 |
|  40 |                [41.2%] LOT-V7-01                                  |
|  30 |                                                                   |
|     +----------------+----------------+----------------+----------------+
|        Jan 12           Feb 02           Feb 23           Mar 29        |
+-------------------------------------------------------------------------+

# 2. Wafer Sort Defect Pareto & Failure Signature Analysis

Initial wafer sort electrical test data collected on Tester 04 (Advantest V93000 platform) across 25 wafers of Lot LOT-V7-001 revealed that electrical fallout was heavily concentrated in two primary software bins:

1. Bin 4 (Digital Core Logic Scan BIST Failure): Accounted for 32.4% of all sorted die (about 55% of total fallout). Dies failed deterministic ATPG scan chains in the embedded 32-bit automotive processing core.

2. Bin 7 (Parametric Analog Leakage / IDDQ): Accounted for 18.1% of all sorted die (about 31% of fallout). Devices exhibited excessive quiescent standby current exceeding the 50 µA specification limit.

3. Bin 2 (Gross Continuity / Open-Short): Accounted for 5.3% of all sorted die (9% of fallout), primarily localized to outer wafer perimeter edge die.

4. Bin 5 (Embedded Flash Memory BIST): Accounted for 3.2% of all sorted die (5% of fallout).

## Spatial Defect Signature

Wafer stacked defect density maps demonstrated a distinct radial signature combined with localized micro-clustering in the central quadrant of the wafers. The outer 15mm exclusion zone exhibited heavy continuity failures, while Bin 4 logic failures mapped directly to regions of high layout pattern density in the arithmetic logic pipeline. Klarf inline inspection files from Penang Fab at post-Metal 3 lithography and etch showed normal particulate levels (<0.04 defects/cm²), indicating that the defect mechanism was introduced downstream during copper metallization and planarization.

Defect Pareto Distribution — First Silicon (Lot LOT-V7-001)

| Defect Mechanism / Bin Classification | Die Count | % Total |
| --- | --- | --- |
| Bin 4: Metal 3 CMP Dishing & Signal Line Bridging | 3,883 | 54.9% |
| Bin 7: High-Voltage IO Rail Leakage / Oxide Stress | 2,169 | 30.7% |
| Bin 2: Wafer Edge Bead Removal (EBR) Open/Short | 635 | 9.0% |
| Bin 5: eFlash Array Charge Pump Marginality | 383 | 5.4% |
| Total Defect Fallout Evaluated | 7,070 | 100.0% |

# 3. Physical Root Cause: Metal 3 Copper CMP Planarization

Deprocessing and destructive physical analysis conducted by Rosa Santos in the Austin FA Lab (refer to internal report FA-2026-0202) confirmed that Bin 4 failures were generated by inter-metal bridging between adjacent Metal 3 copper signal traces.

1. Mechanism of Planarization Failure: The Volta-7 core execution unit incorporates dense parallel 130nm copper routing buses running across Metal 3 with minimum pitch spacing (0.28 µm space / 0.28 µm width). Penang Fab 2 utilizes an automated chemical-mechanical polishing platen utilizing an acidic silica-based slurry.

2. Platen Down-Force & Over-Polish: On Lot LOT-V7-001 through LOT-V7-003, platen down-force was set at 2.8 pounds per square inch (psi) with an extended 15-second soft-pad over-polish intended to clear copper barrier residue (Ta/TaN) from wide bond pad structures.

3. Dishing & Slurry Puddling: Due to local copper density variations exceeding 72% in the core bus region, this aggressive polishing regime induced localized inter-layer dielectric (ILD) erosion (dishing depth >45 nm). Copper barrier slurry pooled into the micro-recesses, leaving residual conductive metallic puddles that created resistive bridges (120 Ω to 1.5 kΩ) between adjacent signal nets.

# 4. Corrective Process Engineering Actions at Penang Fab

Following joint technical reviews between Austin Product Engineering and Penang Fab Operations, an immediate four-point engineering process containment was deployed on January 26, 2026:

1. Down-Force Recipe Modulation: Platen 1 and Platen 2 down-force was reduced from 2.8 psi to 2.1 psi, eliminating excessive pad deflection across high-density metal fields.

2. Slurry Chemistry & Flow Optimization: Switched to a high-selectivity, low-abrasive colloidal silica slurry (Slurry B-4) with an increased chemical inhibitor ratio, suppressing copper removal rates once the Ta barrier layer was exposed.

3. Endpoint Detection Tuning: Transitioned from fixed-time over-polish to advanced optical motor-current endpoint detection (EPD), halting planarization within 2 seconds of barrier clearance.

4. Post-CMP Brush Cleaning & Inline Inspection: Installed a high-pressure megasonic deionized water rinse and integrated an automated brightfield defect inspection gate (KLA 2920) at post-M3 polish with a strict control limit of <12 defect clusters per wafer.

# 5. Yield Recovery Results & Outlook for Rev B Ramp

The implementation of the modified CMP recipe on split lot LOT-V7-004 yielded immediate electrical recovery, jumping from 41.2% to 54.8%. Subsequent baseline lots LOT-V7-006 through LOT-V7-013 demonstrated steady yield consolidation around 56%–58%, with Bin 4 bridging fallout collapsing from 32.4% down to under 6.1%.

However, complete yield entitlement (>75%) on Rev A was constrained by the secondary Bin 7 parametric leakage issue, which was subsequently determined to stem from an undersized ESD clamp in the IO pad ring requiring a silicon metal spin (Rev B). With the fab CMP process fully stabilized and Rev B silicon entering the fab with corrected IO layout geometry, projected wafer sort yield for Q2 2026 is modeled at 78% to 82%, fully meeting NovaDrive Motors' automotive production ramp milestones.