## Slide 1: Volta-7 Reliability Qualification Summary
Author: Kevin Tran, Senior Reliability Engineer
Division: Product Engineering — Quality & Reliability Lab
Date: April 30, 2024

## Slide 2: Title & Executive Qualification Summary
Title: Volta-7 Automotive Reliability Qualification Report (AEC-Q100 Grade 1)
Author: Kevin Tran, Senior Reliability Engineer
Approved By: Anna Becker (Quality Manager), Mike Chen (VP Product Engineering)
Executive Conclusion:
  Volta-7 Rev A silicon failed AEC-Q100 HTOL at 500 hours due to an undersized IO clamp design defect.
  Volta-7 Rev B silicon successfully completed all AEC-Q100 Grade 1 environmental and electrical stress tests.
  FINAL STATUS: FULLY QUALIFIED FOR AUTOMOTIVE PRODUCTION.
Notes: This report presents the definitive reliability dataset for Volta-7. Rev B has cleared all stress tests with zero failures across all sample sets.

## Slide 3: Qualification Methodology & Stress Matrix
Automotive Standard: AEC-Q100 Grade 1 (-40°C to +125°C ambient, TJ = 150°C).
Core Test Matrix (3 Non-Consecutive Lots, 77 Units/Lot, C=0):
  High Temp Operating Life (HTOL): 1000 hrs, TA = 125°C, TJ = 150°C, VDD = 1.15V, VDDIO = 5.25V.
  Temperature Cycling (TC): 1000 cycles, -55°C to +150°C, air-to-air chamber.
  Highly Accelerated Stress Test (HAST): 96 hrs, 130°C, 85% RH, unbiased.
  Preconditioning (Precon): JEDEC MSL3 (192h 30°C/60% RH + 3x reflow at 260°C).
  Electrostatic Discharge (ESD): Human Body Model (HBM) and Charged Device Model (CDM).
Notes: Our test methodology adhered strictly to AEC-Q100 standards, testing devices under extreme accelerated voltage and thermal limits.

## Slide 4: Rev A Qualification Results & HTOL Failure Breakdown
Rev A Stress Test Results Table:
  HTOL (168 Hours): 231 tested, 231 passed (0 fails).
  HTOL (500 Hours): 231 tested, 228 passed, 3 FAILED (Lot LOT-V7-008).
  Temperature Cycling (1000 cyc): 231 tested, 231 passed (0 fails).
  HAST (96 Hours): 231 tested, 231 passed (0 fails).
  HBM ESD: Passed 2.0 kV (marginal on CAN pins).
Failure Analysis Corroboration:
  Units U042, U089, U115 suffered oxide blowout in 120µm IO clamp under sustained DC bias at 150°C.
  Rev A officially designated as FAILED for production use.
Notes: While TC and HAST passed on Rev A, the 3 HTOL failures at 500 hours rendered the silicon unusable for automotive deployment.

## Slide 5: Rev B Qualification Results — Zero Failures
Rev B Qualification Table (Lot LOT-V7-020):
  HTOL (168-Hour Accelerated Screen): 231 tested, 231 passed (0 fails).
  HTOL (1000-Hour Full Qualification): 231 tested, 231 passed (0 FAILS — C=0 ACHIEVED).
  Temperature Cycling (1000 cyc): 231 tested, 231 passed (0 fails).
  HAST (96 Hours): 231 tested, 231 passed (0 fails).
  HBM ESD Robustness: Exceeded >2.5 kV (Passing AEC-Q100 limit).
  CDM ESD Robustness: Exceeded >750 V (Passing AEC-Q100 limit).
Acoustic Microscopy (C-SAM): Zero package delamination post-MSL3 reflow.
Notes: On Rev B, every single unit completed the full stress battery without a single failure or anomaly.

## Slide 6: Parametric Drift & Degradation Analysis
Parametric Stability Across Stress Duration:
  Pin 14 / Pin 22 Leakage Current: Initial: 4.2 nA | Post-500h: 4.8 nA | Post-1000h: 5.1 nA (Limit: <1000 nA).
  Core IDDQ Standby Current: Initial: 14.2 µA | Post-1000h: 15.1 µA (Limit: <50 µA).
  CAN-FD Transceiver Loop Delay: Initial: 112 ns | Post-1000h: 114 ns (Spec: <150 ns).
  Internal Bandgap Reference Drift: Less than 0.12% total shift across -40°C to +150°C.
Statistical Distribution: Pre- and post-stress distribution curves show tight normal Gaussian distribution with zero outlying populations.
Notes: Parametric drift across 1000 hours of HTOL was virtually flat. The 280µm clamp macro provides massive thermal and electrical guardband.

## Slide 7: Final Reliability Sign-off & Recommendation
Formal Sign-off Statement:
  Product Engineering Quality & Reliability certifies that Volta-7 Rev B silicon complies with all AEC-Q100 Grade 1 automotive requirements.
  Zero critical failure modes remain open.
  8D Corrective Action CAR-2024-ND01 (Discipline D6) validated and closed.
Production Recommendation:
  IMMEDIATE UNCONDITIONAL PRODUCTION APPROVAL.
  Ready for NovaDrive Customer Audit presentation on May 12, 2024.
Signatures: Kevin Tran (Lead Reliability Eng), Anna Becker (Quality Mgr), Mike Chen (VP Product Eng).
Notes: Rev B is completely clean. I unreservedly recommend Volta-7 for automotive production release.